CRYSTIC VE679PA

DCPD - Modified Vinyl Ester Resin for Skin Coats

Introduction

Crystic VE679PA is a pre-accelerated, thixotropic, DCPD modified, vinyl ester resin.

Applications

Crystic VE679PA was developed for use as a skin coat in marine and tooling applications.

Features And Benefits

Crystic VE679PA has excellent blister resistance and significantly reduces the occurrence of print through, to produce durable mouldings with an enhanced surface finish.

Approvals

Crystic VE679PA is approved by Lloyd's Register of Shipping for use in the construction of craft under their survey.

Formulation

Crystic VE679PA must be thoroughly stirred and allowed to attain workshop temperature (18°C - 20°C) before use. It needs only the addition of a catalyst to start the curing reaction. Either Butanox LPT or Butanox M50 catalyst can be used, which should be added at 2% into the resin. The geltime of Crystic VE679PA can be approximately determined from the table below.

Pot Life

The resin, mould and workshop should be at, or above, 15C before curing is carried out.

| Temperature | Pot Life in Minutes Using 2% Butanox LPT | Pot Life in Minutes Using 2% Butanox M50 |
| --- | --- | --- |
| 15°C | 50mins | 50mins |
| 20°C | 28mins | 34 mins |
| 25°C | 18mins | 23mins |

Additives

The addition of pigment, fillers or other additives may adversely affect the resin properties. Users should consult Scott Bader’s Technical Service Department before making any such additions.

Properties:

Typical Properties

The following tables give typical properties of Crystic VE679PA when tested in accordance with the appropriate BS or BS EN ISO test method.

| Property |  | Liquid Resin |
| --- | --- | --- |
| Appearance |  | Red / Brown |
| Viscosity at 25C 37.35sec-1 | Poise | 3.5 |
| Viscosity at 25°C 4500sec-1 | Poise | 2.3 |
| Specific Gravity @ 25°C | gcm-3 | 1.065 |
| Stability in the dark at 25C | months | 3 |
| Geltime at 25C using 2% Butanox LPT | minutes | 18 |
| Geltime at 25°C using 2% Butanox M50 | minutes | 23 |

| Property |  | Fully Cured Resin ( unfilled casting ) |
| --- | --- | --- |
|  |  | * ** |
| Barcol Hardness (GYZJ 934 - 1) |  | 23 35 |
| Deflection Temperature under load (1.80 MPa) | °C | 60 94 † |
| Water Absorption 24hrs @23°C | mg | 10 15 |
| Tensile Strength | MPa | 60 52 |
| Tensile Modulus | GPa | 2.7 3.0 |
| Elongation at Break | % | 4.3 2.1 |
| Specific Gravity @ 25°C | gcm-3 | 1.161 1.158 |

*    Curing Schedule - 24hrs @ 20°C, 16hrs @ 40°C

**  Curing Schedule - 24hrs @ 20°C,  3hrs @ 80°C

†    Curing Schedule -  24hrs @ 20°C, 5 hrs @ 80°C, 3 hrs @ 120°C

Storage

Crystic VE679PA should be stored in the dark in suitable closed containers.  It is recommended that the storage temperature should be less than 20°C where practical, but should not exceed 30°C.  Ideally, containers should be opened only immediately prior to use.

Packaging

Crystic VE679PA is supplied in 25kg and 200kg steel containers.

Health And Safety

Please see separate Materials Safety Data Sheet.

Technical Leaflet No. 356.1

Issue Date: March 2005

| Scott Bader Company Limited Wollaston, Wellingborough, Northamptonshire NN29 7RL Telephone: +44 (0) 1933 663100 Facsimile: +44 (0) 1933 665650 |  |
| --- | --- |